## Slide 1: Polytec EC 151-L
Cures at 120 C
Difficult to heat on hot plate, need cover
Very weak connection after cured
  Despite applying a lot of epoxy to hole
  Believe it may be too non-viscous
  Measured 50 Ohm resistance after cured
https://www.intertronics.co.uk/wp-content/uploads/2016/10/Polytec-Electrically_Conductive_Adhesives.pdf

## Slide 2: 8331 Silver Epoxy
Cures at 65 C
Very difficult to apply to headers
  Believe it may be too viscous
  Came out of tube extremely thick
  Believe version we have may be too old
https://www.mgchemicals.com/prcoducts/adhesives/electrically-conductive-adhesives/silver-conductive-epoxy/

## Slide 3: Sn42/Bi57.6/Ag0.4 ChipQuik Solder Paste
Melts at 138 C, reaches 175 C for reflow
Worked according to tests so far
Need to apply a lot
  Much less solder still connected after process
  Do not adjust pin headers until it has cooled
  Look for shiny visual cool before turning off hot plate
  Let bottom of headers be just above hot plate
https://www.chipquik.com/store/product_info.php?products_id=440001
Mounting used: